## Slide 1
Microscopic Ohm’s Law
Outline
Semiconductor Review
Electron Scattering and Effective Mass
Microscopic Derivation of Ohm’s Law

## Slide 2
TRUE / FALSE
Judging from the filled
bands, material A is an
insulator.
2. Shining light on a semiconductor should decrease its resistance.
3. The band gap is a certain location in a semiconductor that electrons are forbidden to enter.
A
B

## Slide 3
1-D Lattice of Atoms
Single orbital, single atom basis
Adding atoms…
  reduces curvature of lowest energy state (incrementally)
  increases number of states (nodes)
  beyond ~10 atoms the bandwidth does not change with crystal size
Decreasing distance between atoms (lattice constant) …
  increases bandwidth

## Slide 4
From Molecules to Solids
Closely spaced energy levels form a “band” of energies between the max and min energies
N-1 nodes
0 nodes
N atoms N states

## Slide 5
Electron Wavepacket in Periodic Potential
Electron wavepacket
Coulomb potential due to nuclei
For smooth motion
  wavepacket width >> atomic spacing
  any change in lattice periodicity ‘scatters’ wavepacket
  - vibrations
  - impurities (dopants)

## Slide 6
Equivalent Free Particle
Electron wavepacket
Coulomb potential due to nuclei
Effective ‘free’ electron wavepacket
Wavepacket moves as if it had an effective mass…
Electron responds to external force as if it had an effective mass

## Slide 7
Name | Symbol | Germanium | Silicon | Gallium Arsenide
Smallest energy bandgap at 300 K | Eg (eV) | 0.66 | 1.12 | 1.424
Effective mass for conductivity calculations |  |  |  | 
Electrons | me*,cond/m0 | 0.12 | 0.26 | 0.067
Holes | mh*,cond/m0 | 0.21 | 0.36 | 0.34
Surprise: Effective Mass for Semiconductors
Electrons wavepackets often have effective mass smaller than free electrons !
Which material will make faster transistors ?

## Slide 8
Approximate Wavefunction for 1-D Lattice
Single orbital, single atom basis
k is a convenient way to enumerate the different energy levels
(count the nodes)
Bloch Functions:
k = π/a
k = 0
k ≠ 0
a
(crystal lattice spacing)

## Slide 9
Energy Band for 1-D Lattice
Single orbital, single atom basis
lowest energy (fewest nodes)
highest energy (most nodes)
Number of states in band = number of atoms
Number of electrons to fill band = number of atoms x 2 (spin)

## Slide 10
From Molecules to Solids
The total number of states = (number of atoms) x (number of orbitals in each atom)
Bands of “allowed” energies for electrons
Bands Gap – range of energy where there are no “allowed states”
r
n = 1
1s energy
n = 2
2s energy
N states
N states

## Slide 11
+e
r
n = 3
n = 2
n = 1
Atom
Solid
Each atomic state  a band of states in the crystal
There may be gaps between the bands These are “forbidden”energies where there are no states for electrons
These are the “allowed” states for electrons in the crystal  Fill according to Pauli Exclusion Principle
Example of Na
Bands from Multiple Orbitals
Z = 11 1s22s22p63s1
What do you expect to be a metal ?
Na? Mg? Al? Si? P?
These two facts are the basis for our understanding of metals, semiconductors, and insulators !!!
Image in the Public Domain
Notes: 11

## Slide 12
Z = 14 1s22s22p63s23p2
4N states
4N states
N states
1s
2s, 2p
3s, 3p
2N electrons fill these states
8N electrons fill these states
Total # atoms = N Total # electrons = 14N
Fill the Bloch states according to Pauli Principle
It appears that, like Na, Si will also have a half filled band: The 3s3p band has 4N orbital states and 4N electrons.
But something special happens for Group IV elements.
By this analysis, Si should be a good metal, just like Na.
What about semiconductors like silicon?

## Slide 13
Antibonding states
Bonding states
4N states
4N states
N states
1s
2s, 2p
3s, 3p
2N electrons fill these states
8N electrons fill these states
The 3s-3p band splits into two:
Z = 14 1s22s22p63s23p2
Total # atoms = N Total # electrons = 14N
Fill the Bloch states according to Pauli Principle
Silicon Bandgap

## Slide 14
Controlling Conductivity: Doping Solids
Boron atom (5)
Silicon crystal
hole
ACCEPTOR DOPING:
P-type Semiconductor
Dopants: B, Al
Silicon crystal
Arsenic atom (33)
Extra electron
DONOR DOPING
N-type Semiconductor
Dopants: As, P, Sb
IIIA
IVA
VA
VIA
Image in the
Public Domain
Conduction
Band
(Unfilled)
Valence
Band
(partially filled)
Conduction
Band
(partially filled)
Valence
Band
(filled)

## Slide 15
Metal
Insulator
or
Semiconductor
T=0
n-Doped
Semi-
Conductor
Semi-
Conductor
T≠0
Making Silicon Conduct

## Slide 16
The bandgap in Si is 1.12 eV at room temperature. What is “reddest” color (the longest wavelength) that you could use to excite an electron to the conduction band?
Typical IR remote control
IR detector
Today’s Culture Moment
Electron
Conduction Band
Hole
Valence Band
Energy
Image is in the public domain
Image is in the public domain

## Slide 17
Semiconductor Resistor
Given that you are applying a constant E-field (Voltage) why do you get a fixed velocity (Current) ? In other words why is the Force proportional to Velocity ?
n
l
A
I
V
How does the resistance depend on geometry ?

## Slide 18
A local, unexpected change in V(x) of electron as it approaches the impurity
Scattering from thermal vibrations
Microscopic Scattering
Strained region
by impurity exerts a scattering force

## Slide 19
Microscopic Transport
vd
Balance equation for forces on electrons:
Drag Force
Lorentz Force
v
t

## Slide 20
Microscopic Variables for Electrical Transport
Drude Theory
Balance equation for forces on electrons:
In steady-state when B=0:
Note: Inside a semiconductor m = m* (effective mass of the electron)
Drag Force
Lorentz Force
and

## Slide 21
Semiconductor Resistor
Recovering macroscopic variables:
OHM’s LAW
and
Start
Finish

## Slide 22
Microscopic Variables for Electrical Transport
For silicon crystal doped at n = 1017 cm-3 :
σ = 11.2 (Ω cm)-1 , μ = 700 cm2/(Vs)and m* = 0.26 mo
At electric fields of E = 106 V/m = 104 V/cm,
v = μE = 700 cm2/(Vs) * 104 V/cm = 7 x 106 cm/s = 7 x 104 m/s
scattering event every 7 nm ~ 25 atomic sites
and
Start
Finish

## Slide 23
Electron Mobility
Electron wavepacket
Change in periodic potential
Electron velocity for a fixed applied E-field
Electron
Conduction Band
Hole
Valence Band
Energy

## Slide 24
Electron Mobility
Intrinsic Semiconductors (no dopants)
  Dominated by number of carriers, which increases exponentially with increasing temperature due to increased probability of electrons jumping across the band gap
  At high enough temperatures phonon scattering dominates  velocity saturation
Metals
  Dominated by mobility, which decreases with increasing temperature

## Slide 25
Key Takeaways
Electron wavepacket
Coulomb potential due to nuclei
Wavepacket moves as if it had an effective mass…

## Slide 26
MIT OpenCourseWare
http://ocw.mit.edu
6.007 Electromagnetic Energy: From Motors to Lasers
Spring 2011
For information about citing these materials or our Terms of Use, visit: http://ocw.mit.edu/terms.